HANGZHOU GARDEN TRADING CO., LTD.

Strand Woven Bamboo Flooring VS Normal Bamboo Flooring

| Name | Unit | The Observation Value with Technological Standard |
| --- | --- | --- |
|  |  | Normal Bamboo Flooring | Strand Woven Bamboo Flooring |
| Static Bending Strength | Mpa | 75.0～100.0 | 125.5～165.5 |
| Hardness | Mpa | 50.0～60.0 | 80.0～120.0 |
| Density | g/cm3 | 0.60～0.75 | 1.0～1.2 |
| Bending or Distortion | ------- | Occurred Often | None |